134	X. Gu et al. / Engineering Fracture Mechanics 160 (2016) 124–137

(a) Striker impacts the incident bar only

(b) Striker impacts the incident and transmitter bar together

Fig. 8. Strain–time curves after impact.

| Striker | Strain gauge | Incident bar |
| --- | --- | --- |
| V |  |  |
| Interfacial zone |  |

Specimen	Strain gauge Transmitter bar

Rigid zone

Fig. 9. Calculation model of PD simulation for SHPB test.

|  | 1.5E-3 |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1.0E-3 |  |  | Reflected wave |  |  |  |  |  |
|  | 5.0E-4 |  |  |  |  |  |  |  |  |  |
| Strain | 0.0E+0 |  |  |  |  |  |  |  |  |  |
|  | 0.0E+0 | 2.0E-4 | 4.0E-4 | 6.0E-4 | 8.0E-4 | 1.0E-3 | 1.2E-3 | 1.4E-3 | 1.6E-3 | 1.8E-3 |
|  | -5.0E-4 | Incident wave |  |  |  | Transmitted wave |  |  |  |
|  | -1.0E-3 |  |  |  |  |  |  |  |  |  |
|  | -1.5E-3 |  |  |  |  |  |  |  |  |  |

time (s)

Fig. 10. Strain–time curve of SHPB test obtained from PD simulation (V = 10 m/s).

In the concrete Brazilian disc SHPB test, the lengths of striker, incident and transmitter bars are 600 mm, 3200 mm and 1800 mm respectively, and the diameter of all 347 stainless steel bars is 74 mm. Measure the strain of two particular points with a distance of 1 m to the specimen in both the incident bar and the transmitter bar. The diameter of the plane Brazilian

| X. Gu et al. / Engineering Fracture Mechanics 160 (2016) 124–137 | 135 |
| --- | --- |

Fig. 11. Progressive failure process of a concrete Brazilian disc in SHPB test. (V = 10 m/s).

Fig. 12. The final cracking patterns of an experiment [38] and the present simulation.

136	X. Gu et al. / Engineering Fracture Mechanics 160 (2016) 124–137

disc is 74 mm. The material parameters of concrete are as follows: Young’s modulus E = 30 GPa, Poisson’s ratio m = 0.25, mass density q = 2400 kg/m3, critical tensile stretch s0 = 0.0018, and critical compressive stretch s0 = 1.0, which is proper for concrete Brazilian test in SHPB. The PD simulation is carried out using the improved PMB model with material point size of |Dx| = 0.0002 m for two-dimensional specimen and |Dx| = 0.0005 m for bars, a horizon size of d = 3|Dx| and a time-step of Dt = 5 10 8 s. The bars are totally discretized into 11,202 material points, while the specimen is discretized into 107,501 material points. The ‘boundary effect’ is mitigated by using the idea of determining the micromodulus constant with its actual integral neighborhood [37].

The peridynamic model is implemented using Fortran90 programming language in Visual Studio 2010, which currently runs only on a single processor computer. It takes approximately 8 h to solve the problem on a Lenovo Intel R CoreTM 4 CPU i5-2400 @ 3.1 GHz desktop computer with 4.00 GB. Fig. 10 shows the strain–time curves measured in the incident bar and transmitter bar with the impact velocity of 10 m/s. The incident wave, transmitter wave and reflected wave can be directly observed and saved.

The damage accumulation and progressive failure process of concrete Brazilian disc in SHPB with 10 m/s impact velocity are shown in Fig. 11. At the initial time of impact loading, a slight damage and fracture occurs in the contact area between concrete Brazilian disc and the incident bar, and between the transmitter bar and the specimen. Then, a main crack starts to initiate, propagate and coalesce from both ends of the specimen to the center along the radial direction. The specimen even-tually splits into two halves. At the same time, large damage areas and many micro-cracks nucleation and propagation occur to dissipate more energy. Fig. 12 shows a comparison between the experimental result [38] and the present simulated result, which are comparable. The simulation reproduces very well the progressive failure of a concrete specimen, and the PD simulation method for SHPB test is proven to be reasonable and applicable as well.

5. Conclusions

In this paper, two types of problems, the elastic wave dispersion and propagation in one dimension, as well as the impact failure of concrete Brazilian disc in SHPB test, are discussed with the bond-based PD. An improved PMB model considering an attenuation function of bond length and an implementation method of the contact-impact process are introduced.

The nonlocal long-range force controls the PD wave dispersion through different material point sizes and horizon sizes. The results demonstrate that the improved PMB model can reduce the numerical dispersion more effectively than the original PMB model and solve one-dimensional elastic wave propagation more accurately than original PMB model, although there is a little dispersion in wave speed. Further, the PD simulation can be used to observe the progressive failure of concrete Brazilian disc and obtain typical cracking patterns. The PD simulation method for SHPB test can be used to analyze the dynamic response of solids suffering impact load.

Although the calculated numerical strain–time curve resembles the measured curve, further verification by experiments is still needed in the future. Since the perfect matching impact between bars in SHPB test barely exists in reality, therefore, the imperfect impact should be another focus of the future studies. In addition, it should be of considerable interest to include the damping and plasticity in the constitutive model to reflect the dynamic response of material subjected to impact loading. Finally, it is also of significance to study the impact failure of Brazilian disc with different pre-existing cracks with our established approaches.

Acknowledgments

This work is financially supported by the National Natural Science Foundation of China (Nos. 11372099, 11132003, 51179064), Jiangsu Provincial Natural Science Foundation (No. BK20151493), National Science and Technology Support Program of China (No. 2015BAB07B10) and the Research Innovation Program for College Graduates of Jiangsu Province (No. KYLX_0420).

References

- Lee OS, Kim MS. Dynamic material property characterization by using split Hopkinson pressure bar (SHPB) technique. Nucl Engng Des 2003;226 (2):119–25.

- Zhao H. Material behavior characterization using SHPB techniques, tests and simulations. Comput Struct 2003;81(12):1301–10.

- Gama BA, Lopatnikov SL, Gillespie JW. Hopkinson bar experimental technique: a critical review. Appl Mech Rev 2004;57(4):223–50.

- Wong LNY, Zou CJ, Cheng Y. Fracturing and failure behavior of Carrara marble in quasistatic and dynamic Brazilian disc tests. Rock Mech Rock Engng 2014;47(4):1117–33.

- Mahabadi OK, Cottrell BE, Grasselli G. An example of realistic modelling of rock dynamics problems: FEM/DEM simulation of dynamic Brazilian test on Barre granite. Rock Mech Rock Engng 2010;43(6):707–16.

- Li XB, Zou Y, Zhou ZL. Numerical simulation of the rock SHPB test with a special shape striker based on the discrete element method. Rock Mech Rock Engng 2014;47(5):1693–709.

- Lanaro F, Sato T, Stephansson O. Microcrack modelling of Brazilian tensile tests with the boundary element method. Int J Rock Mech Min Sci 2009;46 (3):450–61.

- Jiao YY, Zhang XL, Zhao J. Two-dimensional DDA contact constitutive model for simulating rock fragmentation. J Engng Mech 2012;138(2):199–209.

- Silling SA. Reformulation of elasticity theory for discontinuities and long-range forces. J Mech Phys Solids 2000;48(1):175–209.

[10] Silling SA, Epton M, Weckner O, et al. Peridynamic states and constitutive modeling. J Elast 2007;88(2):151–84.

| X. Gu et al. / Engineering Fracture Mechanics 160 (2016) 124–137 | 137 |
| --- | --- |

- Silling SA, Askari E. Peridynamic modeling of impact damage. In: ASME/JSME 2004 pressure vessels and piping conference. American Society of Mechanical Engineers; 2004. p. 197–205.

- Demmie P, Silling SA. An approach to modeling extreme loading of structures using peridynamics. J Mech Mater Struct 2007;2(10):1921–45.

- Ha YD, Bobaru F. Characteristics of dynamic brittle fracture captured with peridynamics. Engng Fract Mech 2011;78(6):1156–68.

- Huang D, Zhang Q, Qiao PZ. Damage and progressive failure of concrete structures using non-local peridynamic modeling. Sci China Technol Sci 2011;54(3):591–6.

- Zhang Q, Gu X, Yv YT. Peridynamic simulation for dynamic response of granular materials under impact loading. Chin J Theor Appl Mech 2016;48 (1):56–63 [in Chinese].

- Tao J. Development and applications of new peridynamic models. Michigan State University; 2012.

- Tao J, Liu D. Simulating wave propagation in SHPB with peridynamics. Dynamic behavior of materials, vol. 1. Springer International Publishing; 2014. p. 195–200.

- Weckner O, Silling SA, Askari A. Dispersive wave propagation in the nonlocal peridynamic theory. In: ASME 2008 international mechanical engineering congress and exposition. American Society of Mechanical Engineers; 2008. p. 503–4.

- Wildman RA, Gazonas GA. A finite difference-augmented peridynamics method for reducing wave dispersion. Int J Fract 2014;190(1–2):39–52.

- Weckner O, Silling SA. Determination of nonlocal constitutive equations from phonon dispersion relations. Int J Multiscale Comput Engng 2011;9 (6):623–34.

- Yu JD, Wang WQ, Li P. Peridynamic modeling of elastoplastic constitutive model. China Mechanical Assembly; 2009 [in Chinese].

- Becker R, Lucas RJ. An assessment of peridynamics for pre and post failure deformation. Army Research Laboratory Aberdeen Proving Ground Maryland Weapons and Materials Research Directorate; 2011.

- Martowicz A, Staszewski WJ, Ruzzene M, et al. Vibro-acoustic wave interaction in cracked plate modeled with peridynamics. In: Proceedings of the WCCM XI, ECCM V, ECFD VI (Barcelona, Spain). p. 20–5.

[24] Martowicz  A. Peridynamics as  an analysis  tool for  wave  propagation  in graphene  nanoribbons. In:  SPIE smart  structures and  materials

+ nondestructive evaluation and health monitoring. International Society for Optics and Photonics; 2015.

- Madenci E, Oterkus E. Peridynamic theory and its applications. Springer; 2014.

- Silling SA, Askari E. A meshfree method based on the peridynamic model of solid mechanics. Comput Struct 2005;83(17):1526–35.

- Kilic B. Peridynamic theory for progressive failure prediction in homogeneous and heterogeneous materials. University of Arizona; 2008.

- Huang D, Lu G, Qiao PZ. An improved peridynamic approach for quasi-static elastic deformation and brittle fracture analysis. Int J Mech Sci 2015;94:111–22.

- Huang D, Lu GD, Wang CW, Qiao PZ. An extended peridynamic approach for deformation and fracture analysis. Engng Fract Mech 2015;141:196–211.

- Bobaru F, Yang M, Alves LF, et al. Convergence, adaptive refinement, and scaling in 1D peridynamics. Int J Numer Meth Engng 2009;77(6):852–77.

- Sau N. Peridynamic modeling of quasibrittle structures. The University of New Mexico; 2008.

- Prakash N, Seidel GD. A novel two-parameter linear elastic constitutive model for bond based peridynamics. In: 56th AIAA/ASCE/AHS/ASC structures, structural dynamics, and materials conference.

- Parks ML, Seleson P, Plimpton SJ, et al. Peridynamics with lammps: a user guide v0. 3 beta. Sandia report SAND2011-8523, Sandia National Laboratories, Albuquerque, NM; 2011.

- Silling SA, Zimmermann M, Abeyaratne R. Deformation of a peridynamic bar. J Elast 2003;73(1–3):173–90.

- Weckner O, Abeyaratne R. The effect of long-range forces on the dynamics of a bar. J Mech Phys Solids 2005;53(3):705–28.

- Weckner O, Emmrich E. Numerical simulation of the dynamics of a nonlocal, inhomogeneous, infinite bar. J Comput Appl Mech 2005;6(2):311–9.

- Ganzenmüller GC, Hiermaier S, May M. Improvements to the prototype micro-brittle linear elasticity model of peridynamics; 2013. Available from: arXiv:1312.5543.

- Zhou ZL et al. Dynamic Brazilian tests of granite under coupled static and dynamic loads. Rock Mech Rock Engng 2014;47(2):495–505.